SYNTHESIS AND CHARACTERIZATION OF THE MICROSTRUCTURE AND FUNCTIONAL GROUP BOND OF Fe3O4 NANOPARTICLES FROM NATURAL IRON SAND IN TOBELO NORTH HALMAHERA

Ferni Malega1, I Putu Tedy Indrayana1*, Edi Suharyadi2

1Physics Study Program, Faculty of Science and Technology Engineering Universitas Halmahera, North Maluku, Indonesia

1Physics Department, Faculty of Mathematics and Science Universitas Gadjah Mada, Yogyakarta, Indonesia

*Corresponding author: tedyindrayana@gmail.com

Received: January 6th, 2018. Accepted: April 2nd, 2018. Published: April 29th, 2018

Abstract: The Fe3O4 nanoparticles have been successfully synthesized from natural iron sand by using co-precipitation method at a temperature of 56oC. The elemental identification, structural characterization, and bonding analysis were carried out by using XRF, XRD, and FTIR, respectively. The sample nanoparticles contain elements of Al, P, Ca, Ti, V, Cr, Mn, Ni, Cu, Zn, Rb, Re, Bi, and Fe. The composition of Fe element is 87.37%. The sample of the nanoparticle exhibited as the Fe3O4 which was shown by the diffraction pattern that belongs to a cubic spinel structure of Fe3O4. The crystallite size of the nanoparticle is 42.25 ± 0.42 nm. The lattice parameter was found at 8.384 ± 0.049 Å. The crystallite density is 5.232103 kg/m3 while the lattice strain is 1.41310-3/line. The FTIR spectra confirm that the existence of Fe-O stretching vibration in the range frequency of 658 cm-1-506 cm-1.

Abstrak: Nanopartikel Fe3O4 telah berhasil disintesis dari pasir besi menggunakan metode kopresipitasi pada suhu 56oC. Karakterisasi sampel Fe3O4 dilakukan menggunakan instrumen XRF, XRD dan FTIR. Spektra XRF menunjukan jenis unsur yang terkandung dalam sampel diantaranya yaitu Al, P, Ca, Ti, V, Cr, Mn, Fe, Ni, Cu, Zn, Rb, Re dan Bi. Komposisi unsur besi Fe sebesar 87,35 %. Sementara itu, pola difraksi sinar-X menunjukan telah terbentuknya fasa Fe3O4 yang memiliki ukuran kristalit (t) rata-rata sebesar 24,25 ± 0,42 nm, nilai parameter kisi kristal (aeks) adalah 8,384 ± 0,049 Å, dan  nilai kerapatan kristal (ρx) sebesar 5,232103kg/m3. Regangan kisi kristal (ε) nanopartikel bernilai 1,41310-3/garis. Spektra FTIR mengkonfirmasi terjadinya absorpsi inframerah pada interval bilangan gelombang 658 cm-1 – 506 cm-1 untuk vibrasi stretching gugus Fe-O pada  subruang kisi oktahedral dan tetrahedral.

© 2018 Pendidikan Fisika FTK UIN Raden Intan Lampung

Kata kunci: Karakterisasi, kopresipitasi, mikrostruktur, pasir besi, sintesis.

INTRODUCTION

Ferrite (MFe2O4) is one group of oxide materials that for three decades has received a lot of attention from researchers to study. This is because ferrite nanoparticles have unique physical properties, including unique mechanical, optical, electrical, acoustic, and magnetic properties compared to other material groups. Ferrite chemical properties such as the stability of chemical reactions and photocatalysis are also unique (Singh & Jaswal, 2014).

Ferrite materials are in various forms, such as nanoparticles, nanoribbons, nanosheets, and nanowires. Nanoparticles are a form of ferrite material in the form of particles with various morphologies, for example like solid balls.

One example of ferrite nanoparticles is magnetite (Fe3O4). The Fe3O4 nanoparticles consist of divalent cation Fe2+ and trivalent Fe3+ cations. This nanoparticle has an inverse spinel crystal structure with the formula of cation distribution that is (Fe3+)tet [Fe2+ Fe3+]octa O2-4 (Varma & Rani, 2015). The geometry of the crystal structure of Fe3O4 nanoparticles can be illustrated in Figure 1.

Figure 1. Crystal structure invers spinel Fe3O4: (a) crystal structure of Fe3O4, (b) octahedral and tetrahedral sub lattice structures (Motoro, 1938)

Based on its physical and psycho-chemical properties, the Fe3O4 nano-particles have various potential applications. In medical field, the Fe3O4 can be used as a contrast agent for MRI images, drug delivery agents, and cancer thermotherapy agents. In the environmental field, the Fe3O4 can be used as catalysis to reduce organic and inorganic compounds found in contaminated liquid substances. In this field, the Fe3O4 can also be used as a magnetic adsorbent for dissolved heavy metal ions in a liquid (Li et al., 2006; Xu et al., 2012; Tang et al., 2013). In the field of electronics and instrumentation, the Fe3O4 can be applied as the main material in the manufacture of inductor coils, electromagnetic wave coating materials, and microwave absorber (Valenzuela, 2012).

The superior physical and chemical properties of Fe3O4 nanoparticles are influenced by various factors, such as microstructure, grain morphology structure and particle size (Cui et al., 2011). Microstructure factors include crystal structure, length of crystal lattice parameters, lattice defects, and crystal density, including the various phases of the nanoparticles. The microstructure factor is influenced by several factors, namely the type of starting material, synthesis method, precursor mole composition, synthesis temperature, and additional heat treatment such as annealing, sintering, or calcination (Ring et al., 2013).

Various methods have been used to synthesize Fe3O4 nanoparticles, such as coprecipitation (Sun et al., 2009; Cui et al., 2011; Ring et al., 2013; Qu et al., 2013) thermal decomposition and metal reduction reactions (Darminto et al., 2008). The coprecipitation method is the easiest chemical method to do compared to other methods because the co-precipitation method does not involve a high synthesis temperature (> 150oC), a long synthesis time, and the process is not complicated (Nuzully et al., 2013).

The use of coprecipitation method in the synthesis of Fe3O4 nanoparticles involves precursors in the form of anhydrous metal salt compounds (metal salt), such as FeCl3.6H2O as providers of Fe3+ and FeCl2.4H2O cations as providers of Fe2+, or Fe2SO4.6H2O cations as Fe2+ providers (Darminto et al., 2011; Sartika et al., 2014). The anhydrous synthetic compounds can be replaced with natural materials such as iron sand containing Fe2+ and Fe3+ metals. Several studies have succeeded in synthesizing Fe3O4 nanoparticles using natural materials of iron sand, such as (Darminto et al., 2008; Darminto et al., 2011; Bilalodin et al., 2013; Setiadi et al., 2016; Taufiq et al., 2017).

In this research, Fe3O4 nanoparticles will be synthesized from natural materials of iron sand found in Wari Ino Beach, Tobelo Subdistrict, North Halmahera as precursors in providing Fe2+ and Fe3+ ions. The availability of iron sand in Wari Ino Beach is very abundant and until now there has been no research that covers the metal mineral content of iron Fe2+ and Fe3+, especially using it as a base for a synthesis of Fe3O4 nanoparticles. Information about the mineral content of iron sand is very interesting to study and the process of synthesizing Fe3O4 nanoparticles using iron sand needs to be done in the framework of its application needs for various applied fields, especially the environment. Microstructure studies of Fe3O4 nanoparticles from iron sand are important to be carried out in order to provide empirical justification of their physical and chemical properties.

This study focuses on the synthesis and microstructure studies of Fe3O4 nanoparticles including crystal structure, lattice parameters (lattice parameters), crystal spacing, X-ray density, lattice strain and texture coefficient.

RESEARCH METHOD

1. Apparatus and Materials

The apparatus used to synthesize Fe3O4 nanoparticles are 250 ml beaker, 100 ml beaker, spatula rod, drop pipette, pour bottle, petri dish, magnetic hot plate, oven, thermometer, pH meter and digital scales. While the characterization tool is used by XRF, XRD and FTIR instruments. The material used for the synthesis of Fe3O4 nanoparticles is iron sand, HCl, NaOH and distilled water.

2. Sample Preparation Procedure

The synthesis process of Fe3O4 nanoparticles can be illustrated such as Figure 2. The process was started by dissolving iron sand (total mass of 10 grams) into 20 ml HCl (6M) and stirred while heating at 70oC for 30 minutes on a hot plate stirrer with the aim of forming a solution of FeCl3 and FeCl2. A total of 3.0 grams of NaOH were dissolved in 20 ml of distilled water. The NaOH solution was heated for 10 minutes after being sterilized for 15 minutes. The solution which is formed from the result of a mixing of iron sand with HCl is then taken as much as 20 ml. The iron sand solution is dropped into NaOH solution using a dropping pipette while being sterilized and heated with a synthesis temperature of 56oC.

Figure 2. Process of synthesis of Fe3O4 samples.

After a hour of the synthesis process, black deposits (slurry) will form. The temperature of this precipitate is naturally derived until it reaches thermal equilibrium with room temperature. The precipitate was rinsed with distilled water and deposited again on a permanent magnet for 30 minutes. The rinsing process is carried out five times, every time the rinsing process is carried out in pH measurements. The precipitate is then in the oven at a temperature of 100oC for 3 hours. This slurry heating process will produce solid pieces which are a collection of Fe3O4 nanoparticles. The chips are crushed to produce nanoparticle powder (Figure 2) which is further characterized.

3. Characterization of Nanoparticles

The elemental composition of the samples was identified using X-ray fluorescence (XRF) instrument. Characterization of a microstructure of nanoparticles including crystal structure, lattice parameters, crystal spacing distance, X-ray density, lattice strain and texture coefficient was carried out using X-ray diffractometer (X-ray diffractometer- XRD). Nanoparticle functional groups were characterized using Fourier -FTIR transformed infrared spectrophotometer.

RESULTS AND DISCUSSION

1. Qualitative Description of Fe3O4 Nanoparticles

Sample obtained from the synthesis of Fe3O4 nanoparticles in the form of fine black powder. Black color is one of the characteristics of Fe3O4 nanoparticles. In addition, other characteristics have also been observed, namely the response of powder nanoparticles when tested with an external magnet. Powder nanoparticles experience a magnetic attraction to external magnets.

2. The Elemental Composition of Fe3O4

The XRF characterization results of Fe3O4 nanoparticle samples provide information regarding the type and composition of the elements contained in the sample. The types of these elements are determined based on characteristic X-ray energy radiated by the atoms contained in the material. Meanwhile, the element composition is indicated by the peak height of the spectra as shown in Figure 3.

The XRF spectra confirmed the presence of fourteen types of elements contained in Fe3O4 nanoparticle samples, namely aluminum (Al), phosphorus (P), calcium (Ca), titanium (Ti), vanadium (V), chromium (Cr), manganese ( Mn), Iron (Fe), Nickel (Ni), copper (Cu), Zinc (Zn), Rubidium (Rb), rhenium (Re) and bismuth (Bi) are presented in Table 1.

Figure 3. The XRF Spectra of Fe3O4 nanoparticles.

According to the results, the most elemental content is iron (Fe) with an elemental composition of 87.35%, while the least elemental content is zinc (Zn) with an elemental composition of 0.08%. The composition of Fe metal in the sample results of this study is greater than the results obtained by Darminto et al (2011); Bilalodin et al (2013) and Kartika and Pratapa (2014). Darminto et al (2011) used the coprecipitation synthesis method at 80oC for a hour and produced Fe3O4 samples with Fe content of 76.92%. Bilalodin et al (2013) obtained an Fe content of 21.00%. Meanwhile, Kartika and Pratama (2014) using the dissolved metal method of hydrochloric acid produced Fe3O4 samples with Fe composition of 87.00%. The difference in results can be caused by differences in synthesis methods and synthesis parameters used in producing Fe3O4 nanoparticles. Therefore, the selection of the right synthesis method and the value of the synthesis parameter is very influential mainly on the composition and physical properties of Fe3O4 produced.

Table 1. Elemental composition of sample

| No | Element | Composition (%) |
| --- | --- | --- |
| 1 | Al | 1.00 |
| 2 | P | 0.26 |
| 3 | Ca | 0.61 |
| 4 | Ti | 4.73 |
| 5 | V | 0.63 |
| 6 | Cr | 1.75 |
| 7 | Mn | 0.56 |
| 8 | Fe | 87.35 |
| 9 | Ni | 1.34 |
| 10 | Cu | 0.14 |
| 11 | Zn | 0.08 |
| 12 | Rb | 0.46 |
| 13 | Re | 0.20 |
| 14 | Bi | 0.68 |

Based on the results in Table 1, the Fe3O4 nanoparticles still contained impurities such as Al, P, Ca, Ti, V, Cr, Mn, Ni, Cu, Zn, Rb, Re, and Bi. This states that the process of separating magnetic iron material with nonmagnetic elements has not yet occurred optimally. The existence of these elements does not significantly affect the physical and psycho-chemical properties of Fe3O4 nanoparticles.

3. The Microstructural properties of Fe3O4

X-ray diffraction test was carried out to identify the microstructure and crystal structure of Fe3O4 nanoparticles which included crystallite size, lattice parameters, crystal density, lattice strain and texture coefficient. X-ray diffraction data of Fe3O4 samples were adjusted to the standard data of Joint Committee Powder Diffraction Standard (JCPDS) no. 11-0614.

The X-ray diffraction test results of Fe3O4 nanoparticles give data in the form of 2θ diffraction angle and intensity. The diffraction pattern was plotted by using Origin 9.0 for Windows software as shown in Figure 4. The diffraction pattern shows the existence of seven diffraction peaks. The seven diffraction peaks state the electron diffraction process that occurs in the diffraction (hkl) plane of Fe3O4 nanoparticles, namely fields (220), (311), (400), (422), (511), (440), and (533) which are characteristics of Fe3O4 nanoparticle diffraction pattern according to JCPDS standard data 11-0614. In this diffraction pattern, no diffraction peaks were found in phases other than Fe3O4, so it can be concluded that the pure synthesized samples consisted of Fe3O4 nanoparticles.

The calculation results of the crystal lattice of Fe3O4 nanoparticle approach the standard value according to JCPDS number 11-0614, which is 8.34 ± 0.049 Å. This value is equivalent to the results of research by Darminto et al (2011), Setiadi et al (2016) and the standard value of the JCPDS data is 8.396 Å. The volume of the Fe3O4 crystal lattice is 0.58910-27 m3. The average size of Fe3O4 nanoparticles is 24.25 ± 0.042 nm. The crystal lattice density (ρx) Fe3O4 is 5.232103 kg/m3 and the strain value that occurs in the lattice (ε) is 1.41310-3 /line.

Figure 4. The XRD pattern of Fe3O4 nanoparticles.

The degree of crystallinity of Fe3O4 samples can be identified based on data of texture coefficient (TC) of relating diffraction peak (hkl). Figure 5 shows TC value (hkl) for each orientation direction of Fe3O4 nanoparticles crystal grains. The results of calculation of TC values (hkl) diffraction peaks in fields (220), (311), (400), (422), (511), (440) and (533) respectively (0.9), (2, 3), (0.7), (0.4), (0.8), (1.2) and (0.6). From the calculation of the TC (hkl) value there are five diffraction peaks which have a TC value (hkl) smaller than 1 of them namely the diffraction peaks of the fields (220), (440), (422), (511) and (533) indicates that the growth of Fe3O4 nanoparticles at the diffraction peak tends to be very low and the direction of the crystal grain orientation is not regular

Figure 5. Texture coefficient of the XRD peaks of Fe3O4 nanoparticle.

4. Functional Groups Bonds of Fe3O4

The Fourier Transform Infrared Spectroscopy (FTIR) test results provide information about the infrared spectra absorption profile on Fe3O4 nanoparticle samples. Characterization of Fe3O4 nanoparticles FTIR was carried out for the 500 cm-1- 4000 cm-1 wavenumber interval. The data plot transmits the wave number of infrared light in the form of sharp absorption peaks in certain wavenumbers resulting from the vibration of certain functional groups, as shown in Figure 6 and Table 2.

The stretching vibration of Fe-O functional groups occurs for absorption of infrared wavenumbers in the range 506 cm-1- 658 cm-1. These results are consistent with the findings of Setiadi et al (2016). In the wave number interval 1672 cm-1 - 1367 cm-1 it is identified the occurrence of bending vibration of the H-O-H group, while the O-H group vibrates stretching at a wave number interval of 3028 cm-1- 3400 cm-1. At wave number interval 2920 cm-1 - 2855 cm-1, stretching vibration of C-H group is identified.

Figure 6. The FTIR Spectra of Fe3O4 nanoparticle.

Table 2. Functional group bonds of  Fe3O4 nanoparticles.

| No. | Wavenumber (cm-1) | Functional group |
| --- | --- | --- |
| 1 | 658 – 506 | Fe – O stretching |
| 2 | 1672 – 1367 | H – O – H bending |
| 3 | 3028 – 3400 | O – H stretching |
| 4 | 2920 – 2855 | C – H stretching |

CONCLUSION

The Fe3O4 nanoparticles have been successfully synthesized using the coprecipitation method at 56oC. The Fe3O4 samples synthesized from the iron sand of Wari Ino Beach contain elements of Fe at 87.35%. The Fe3O4 nanoparticles have a spinel cubic crystal structure. The average crystallite  size (t) of Fe3O4 nanoparticles was 24.25 ± 0.42 nm and the crystal lattice (aex) parameter value was 8.34 ± 0.049 Å. The appearance of stretching vibration of the Fe-O functional group at a wave number of 658 cm-1 - 506 cm-1 also shows the success of the formation of Fe3O4 nanoparticles.

ACKNOWLEDGMENTS

The author would like to thank the staff of Laboratorium IPA Terpadu Universitas Halmahera for providing opportunities using the research facilities, staff of the Mineral Laboratory and Advanced Materials of the Mathematics and Natural Sciences Faculty of Malang State University which helped provide facilities for characterizing Fe3O4 nanoparticles, as well as the Magnetic Nanomaterial Research Group UGM for providing the materials.

REFERENCES

Bilalodin, Sunardi & Effendy, M. (2013). Analisis Kandungan Senyawa Kimia dan Uji Sifat Magnetik Pasir Besi Pantai Ambal. Jurnal Fisika Indonesia, 17(50), 35 – 40.

Cui, W., Ling, L.J., Cai, L.D., ShaoLan, Z., & HongChao, C. (2011). Analysis of the Factors Affecting the Magnetic Characteristics of Nano-Fe3O4 Particles. Chinese Science Bulletin: Material Science, 56 (8), 803 – 810.

Darminto, Pratapa, S & Taufiq, A. (2008). Sintesis Partikel Nano Fe3-xMnxO4 Berbasis Pasir Besi dan Karakterisasi Struktur serta Kemagnetannya. Jurnal Nanosains & Nanoteknologi, 1(2), 67 – 73.

Darminto, Yahya, E., Triwikantoro & Mashuri. (2011). Synthesis of Fe3O4 Nanoparticles from Iron Sands and Effects of Ni and Zn Substitution on Structures and Magnetic Properties. Journal of Materials Science and Engineering A, 1, 182 – 189.

Li, M., Fan, M., Brown, C., Van Leeuwen, J., Wang, J., Wang, W., Song, Y & Zhang, P. (2006). Synthesis, Properties, and Environmental Appli-cations of Nanoscale Iron-Based Materials: A Review. Critical  Review on Environment Science and Technology, 36, 405–431.

Motoro, V. (1938). Miscibilita Fra Gli Ossidi Salini di Ferro e di Manganese. Gazzetta Chimica Italiana, 68, 728 – 733.

Nuzully, S., Kato, T., Iwata, S  & Suharyadi, E. (2013). Pengaruh Konsentrasi Polyethylene glycol (PEG) pada Sifat Kemagnetan Nanopartikel Magnetik PEG-Coated Fe3O4. Jurnal Fisika Indo-nesia,17(51), 35 – 40.

Qu, S., Wei, Q & Wang, B. (2013). Synthesis and Characterization of Uniform and Crystalline Magnetite Nanoparticles via Oxidation-precipitation and Modified Co-precipitation Methods. International Journal of Electrochemical Science, 8, 3786 - 3793.

Hankare, P.P., Jadhav, S.D., Sankpal, U.B., Chavan, S.S., Waghmare, K.J, & Chougule, B.K. (2009). Synthesis, Characterization, and Effect of Sintering Temperature on Magnetic Properties of MgNi Ferrite Prepared by Coprecipitation Method. Journal of Alloys and Compounds, 475, 926 - 929.

Ring, T.A., Pei., Y & Mascolo, M.C. (2013). Room Temperature Co-Precipitation Synthesis of Magnetite Nanoparticles in a Large pH Window with Different Bases. Materials, 6, 5549 – 5567.

Sartika, D., Puji A, F & Suharyadi, E. (2014). Studi Penurunan Kadar Logam Fe dan Co pada Limbah Cair dengan Sistem Purifikasi Berbasis Adsorben Nanopartikel Magnetik Fe3O4. Jurnal Fisika Indonesia, 18 (52), 16 – 19.

Setiadi, E.A., Sebayang, P., Ginting, M., Sari, Y.A., Kurniawan, C., Saragih, C.S & Simamora, P. (2016). The Synthesization Of Fe3O4 Magnetic Nanoparticles Based on Natural Iron Sand by Co-Precipitation Method for the Used of the Adsorption of Cu and Pb Ions. Journal of Physics: Conference Series, 776, 1 – 6.

Singh, B & Jaswal, L. (2014). Ferrite materials: A Chronological Review. Journal of Integrated Science and Technology, 2(2), 69 - 71.

Sun, S., Frey, N.A., Peng, S & Cheng, K. 2009. Magnetic Nanoparticles: Synthesis, Functionalization, and Applications in Bioimaging and Magnetic Energy Storage. Chemistry Society Review, 38(9), 2532 – 2542.

Tang, S.C.N & Lo, I.M.C. (2013). Magnetic Nanoparticles: Essential Factors for Sustainable Environ-mental Applica-tions. Water Research, 47, 2613-2632.

Taufiq, A., Saputro, R.E., Sunaryono, Hidayat, N., Hidayat, A., Mufti, N., Diantoro, M., Patriati, A., Mujamilah, Putra, E.G.R & Nur, H. (2017). Fabrication of Magnetite Nano-particles Dispersed in Olive Oil and Their Structural and Magnetic Investigations. IOP Conf. Series: Materials Science and Engineering, 202, 1 – 8.

Valenzuela, R. (2012). Novel Applications of Ferrites: Review Articles. Physics Research International, 5(9), 183 – 189.

Varma, G.D & Rani, S. (2015). Superparamagnetism and Metamag-netic Transition in Fe3O4 Nanoparti-cles Synthesized via Co-Precipitation Method at Different pH. Physica B, 472, 66 – 77.

Xu, P., Zeng, G.M., Huang, D.L., Feng, C.L. Hu, S., Zhao, M.H., Lai, C.,  Wei, Z.,  Huang, C., Xie, G.X & Liu, Z.F. (2012). Use of Iron Oxide Nanomaterials in Wastewater Treat-ment: a Review. Science Total Environmental, 424, 1–10.

# Text boxes

(a)

(b)

Fe3O4

Nanoparticles